## Slide 1
Moisture, acids,
Environmental Conditions
Copper containing materials
Type equation here.

## Slide 2
20 µm
20 µm
(a)
(b)
(c)
(d)

## Slide 3
0
10
20
30
40
Ti6Al4V
Ti-Al-V-Cu
Live: Green Fluorescence
Em = 505 nm [a.u.]
LIVE
E. coli live / dead assay, 24 h
*

## Slide 4
Ti6Al4V
Ti-Al-V-Cu
Dead: Red Fluorescence
Em = 635 nm [a.u.]
DEAD
E. coli live / dead assay, 24 h
*
0
1
2
3

## Slide 5
(d)
(c)
Dendritic structure
10 µm
1 µm
(b)
(a)

## Slide 6
Slurry
spray coating
(a)
Samples
Control Panel
Laser Head
Scan Direction
Ti6Al4V
x
z
y
(b)
(c)
(d)
Imax=26.9 kW/mm2
200 mm/s
+
PVA
micro-nano Cu particles

## Slide 7
Slurry spray coating
(a)
Samples
Control Panel
Laser Head
Scan Direction
Ti6Al4V
x
z
y
(b)
(c)
(d)
200 mm/s
Imax=26.9 kW/mm2
+
PVA
micro-nano Cu particles

## Slide 8
(a)
(c)
(b)
(d)

## Slide 9
6.84 ms
21.3 ms
39.1 ms
0.42 ms
12.8 ms
27.4 ms
T [K]
(a)
(b)
(c)

## Slide 10
t=12ms
t=875ms
t=5000ms
x
y
(a)
(b)
(c)
(d)

## Slide 11
(a)
(b)

## Slide 12
Alloyed layer
(c)
Lamellar structure
Precipitates
(ω-phase)
(d)
(a)
(b)

## Slide 13
Alloyed layer
(c)
Lamellar structure
Precipitates
(ω-phase)
(d)
2
Intensity [a.u]
Ti-
Ti-
Ti2Cu
(a)
(b)

## Slide 14
Ti6Al4V
Ti-Al-V-Cu
0
50
100
150
200
Positive signals [% of pixels]
20 µm
20 µm
(a)
(b)
(c)

## Slide 15
Ti6Al4V
Imax=26.9 kW/mm2
t=5000ms
FEA
Microstructure
Phase – field simulation
Anti-Bacteria
Laser Manufacturing
Cu powder bed
Vs=200mm/s
HETEROGENEOUS
STRUCTURES
BIOMATERIALS
SUPER-GAUSSIAN
HEAT SOURCE
INTERFACE
MODELING

## Slide 16
20
40
60
80
100
(i) Ti-Al-V-Cu
(ii) Ti6Al4V
(iii) Cu powder
Ti-
Ti-
Ti2Cu
2
Intensity [a.u]
(022)
(002)
(111)

## Slide 17
2
Intensity [a.u]
Ti-
Ti-
Ti2Cu
20
40
60
80
100
(i) Ti-Al-V-Cu
(ii) Ti6Al4V
(iii) Cu powder
Ti-
Ti-
Ti2Cu
2
Intensity [a.u]
(022)
(002)
(111)